BN® BL4109

Twill Floor Vinyl

Description ：

Film：     170 micron transparent twill PVC film

Adhesive： transparent adhesive

Liner：    100gsm white PEK paper with one side PE& silicon coating

Width：   1.06/1.27/1.37/1.52m

Features：

1.  Anti-skidding, anti-friction, image protection and stereoscopic effect;

2.  Excellent flatness and anti-shrinkage, easy to clean and good picture appearance;

Applications：

The products are mainly used for picture protection (such as Floor guide signs, indoor floor advertising cold mounted), and also plays a role of anti-skid

Technical Data：

Testing condition: Indoor temperature 23±2℃; Relative humidity 50±5%; Use aluminum, glass, steel plate as the base material for testing.

| Test Items | units | Test method | Average value |
| --- | --- | --- | --- |
| Thickness PVC Weight-liner Weight -finished product Initial adhesive 24h，180°peel Dimensional stability MD Dimensional stability CD Tensile strength MD Tensile strength CD Construction temperature Applicable temperature | Micron g/m² g/m² N/25mm N/25mm mm mm N/25 mm N/25 mm ℃ ℃ | GB/T6672-2001 GB4669-1995 GB4669-1995 FTM 9 FTM 1 FTM 14 FTM 14 GB/T1040.1-2006 GB/T1040.1-2006 | 170±10 100±10 310±20 ≥5 ≥8 ≤1.8 ≤1.5 ≥50 ≥60 20±10℃ -20～+70 |

- All technical data is subject to change without prior notice

Storage Condition：

All NAR products always need to be stored in the original packing and with the original protection materials, preferably stored hermetically, no more than 6 layers if stored horizontally. Do not expose in direct sunlight or heat sources. Shelf life will be one year with temperature of 25°C±5°C and relative humidity of 50±15%.

Production and Application Environment：

Production environment: Production environment: temperature of 25 ± 5 °C, relative humidity of 50%±10%, clean dust-free environment without suspended matter; Begin the cold lamination and other operation after the image is complete dry.

Application environment: temperature of 20±10°C, relative humidity of 50±10%; Pasting on flat, smooth and clean surface without floating dust and shedding; It is necessary to take more than 2 hours for maintenance before laminating.

Warranty Condition：

1.  One year shelf life: stored in suitable conditions, preferably use within 6 months;

2.  One year prosecution period: from the product manufacture date, no-acceptance for overdue product.

Important Remark：

The information mentioned in this product data sheet is based upon tests that were executed by NAR, and that we consider to be reliable. The information always represents an average, a minimum or a maximum value. It is only give for your information, and does not give any guarantee. It is up to the end user to decide whether or not the product is suitable for the particular application.

Product Application：