IV7511

Blended Modified POE Composite lnkjet Material

Description：

Film:       80 micron; POE composite material

Adhesive：  Removable grey solvent adhesive

Liner：     120 gsm white PEK paper with one side PE & Silicon coating

Width：    1.06/1.27/1.37/1.52m

Features：

- The good dimensional stability of the surface material, no curling or warping;

2.  Product substrate toughness, good stiffness, easy for construction

3.  The fast speed ink absorption and good color reducibility;

4.  High pixel return point ratio, suitable for high-precision images;

5.  Resistant to UVA-340 UV light, and energy radiation 0.55 w/m2, 200 hours color difference change valueΔ<4;

Application：

- Applicable to Vehicle flat surface decoration, Billboards, indoor and outdoor advertising;

- Suitable for various of solvent, Eco solvent and UV;

Technical Data

Test Condition：Indoor temperature 23±2℃,Relative Humidity 50±5%.

Test tools like Aluminum plate, glass, steel plate are used for below testing .

| Test Items | units | Test method | Average value |
| --- | --- | --- | --- |
| Thickness PVC Weight-liner Weight-finished product Gloss Rate 60° Primary adhesive 24h, 180°peel Dimensional stability MD Dimensional stability CD Tensile strength MD Tensile strength CD Construction Temperature Applicable Temperature | Micron g/m² g/m² % N/25mm N/25mm mm mm N/25 mm N/25 mm ℃ ℃ | GB/T6672-2001 GB4669-1995 GB4669-1995 GB8807-88 FTM 9 FTM 1 FTM 14 FTM 14 GB/T1040.1-2006 GB/T1040.1-2006 | 80±10 120±10 290±20 ≤15 ≥2 ≥4 ≤1.0 ≤1.0 ≥50 ≥40 20±10℃ -20～+70 |

*All technical data is subject to change without prior notice

Storage Condition：

All NAR products should be stored in the original packaging with original protective materials, it is recommended to seal storage, horizontal storage, stacking layer should not exceed 6, avoid direct sunlight, heat source direct contact. Storage temperature 25±5℃, relative humidity 50±15%. Under these conditions, the storage period of the product is 6 months.

Printing Environment：

Production environment: temperature of 25±5°C, relative humidity of 50%±10%, clean dust-free environment without suspended matter; please move the materials to the printing environment 24 hours before printing. Test prior to use and remain enough edge margins when printing.

Application environment: temperature of 20±10°C, relative humidity of 50±10%; Pasting on flat, smooth and clean surface without floating dust and shedding; It is necessary to take more than 2 hours for maintenance before laminating.

Warranty：

1.  One year shelf life: stored in suitable conditions, preferably use within six months.

2.  One year prosecution period: from the product manufacture date, no-acceptance for overdue product.

Important Remark：

- The information mentioned in this product data sheet is based upon tests that were executed by NAR, and that we consider to be reliable. Environment humidity more than 70% in different district will decrease the printing result.

- This product is with removable glue and has the possibility of residual gum with different substrate and pasting period. It is not recommended to splice different batches of products.

Product Application：

※Shanghai Yifeng Square：