NO3609T

Tri-Layer One Way Vision

Description：

Film:      140micron; black & white PVC film

Adhesive： transparent adhesive

Liner：   75gsm perforated paper+70gsm PEK paper

Width：   1.06/ 1.27/1.37/1.52m

Features：

1.  One side visual, sun-shade and privacy protection; Hole size 1.40mm, perforation 30%;

2.  Stable ink absorption and excellent dimensional stability;

Applications：

- Applicable to glass surface, also applicable to transparent acrylic, PVC, PET transparent panels;

- This product is recommended to use UV printing; Also suitable for various solvent ink and Eco-solvent ink.

Technical Data：

Testing condition: Indoor temperature 23±2°C; Relative humidity 50±5%; Use aluminum, glass, steel plate as the base material for testing.

| Test Items | Units | Test method | Average value |
| --- | --- | --- | --- |
| Thickness PVC Weight-Liner Weight -finished product 24h, 180°peel Dimensional stability MD Dimensional stability CD Tensile strength MD Tensile strength CD Construction Temperature Applicable Temperature | Micron g/m² g/m² N/25mm mm mm N/25 mm N/25 mm ℃ ℃ | GB/T6672-2001 GB4669-1995 GB4669-1995 FTM 1 FTM 14 FTM 14 GB/T1040.1-2006 GB/T1040.1-2006 | 140±10 130±10 290±20 ≥4 ≤1.5 ≤1.0 ≥25 ≥20 20±10 -20 ~ +70 |

* All technical data is subject to change without prior notice.

Storage Condition：

All NAR products always need to be stored in the original packing and with the original protection materials, preferably stored hermetically, no more than 6 layers if stored horizontally. Do not expose in direct sunlight or heat sources. Shelf life will be one year with temperature of 25°C±5°C and relative humidity of 50±15%.

Production and Application Environment：

Production environment: temperature of 25±5°C, relative humidity of 50%±10%, clean dust-free environment without suspended matter; Please move the materials to the printing environment 24 hours before printing. Test prior to use and remain enough edge margins when printing.

Application environment: temperature of 20±10°C, relative humidity of 50±10%; Pasting on flat, smooth and clean surface without floating dust and shedding; It is necessary to take more than 2 hours for maintenance before laminating.

Warranty Condition：

1.  One year shelf life: stored in suitable conditions, preferably use within 6 months;

2.  One year prosecution period: from the product manufacture date, no-acceptance for overdue product.

Important Remark：

The information mentioned in this product data sheet is based upon tests that were executed by NAR, and that we consider to be reliable. Environment humidity more than 70% in different district will decrease the printing result.

Product Application：