NV6002-1

Backlit Self Adhesive Vinyl

Description：

Film:       100 micron; glossy PVC film

Adhesive：  Clear adhesive

Liner：     140gsm one side PEK liner

Width：    1.27/1.37/1.52m

Features：

1.  High performance film, stable ink absorption, bright colors, vivid images.

2.  It can be applied on the light box

3.  Stable glue performance, easy application to a wide variety of substrates.

Applications：

- Applicable to light box

- Suitable for various solvent ink, Eco-solvent ink and UV ink

Technical Data：

Testing condition: Indoor temperature 23±2°C;Relative humidity 50±5%;Use aluminum, glass, steel plate as the base material for testing.

| Test Items | Units | Test method | Average value |
| --- | --- | --- | --- |
| Thickness PVC Weight-Liner Weight -finished product Gloss Rate 60° Initial Adhesion 24h, 180°peel Dimensional stability MD Dimensional stability CD Tensile strength MD Tensile strength CD Construction Temperature Applicable Temperature | Micron g/m² g/m² % N/25mm N/25mm mm mm N/25 mm N/25 mm °C °C | GB/T6672-2001 GB4669-1995 GB4669-1995 GB8807-88 FTM 9 FTM 1 FTM 14 FTM 14 GB/T1040.1-2006 GB/T1040.1-2006 | 100±10 140±10 300±20 ≥60 ≥8 ≥10 ≤1.2 ≤1.0 ≥40 ≥35 20±10°C -20 ~ +70 |

- All technical data is subject to change without prior notice.

Storage Condition：

All NAR products always need to be stored in the original packing and with the original protection materials preferably stored hermetically, no more than 6 layers if stored horizontally. Do not expose in direct sunlight or heat sources. Shelf life will be one year with temperature of 25°C±5°C and relative humidity of 50±15%.

Production and Application Environment：

Production environment: temperature of 25±5°C, relative humidity of 50%±10%, clean dust-free environment without suspended matter; Please move the materials to the printing environment 24 hours before printing. Test prior to use and remain enough edge margins when printing.

Application environment: temperature of 20±10°C, relative humidity of 50±10%; Pasting on flat, smooth and clean surface without floating dust and shedding; It is necessary to take more than 2 hours for maintenance before laminating.

Warranty Condition：

1.  One year shelf life: stored in suitable conditions, preferably use within six months. Quality range is only for ink adsorption, other physical parameter is only for reference.

2.  One year prosecution period: from the product manufacture date, no-acceptance for overdue product.

Important Remark：

- The information mentioned in this product data sheet is based upon tests that were executed by NAR, and that we consider to be reliable. Environment humidity more than 70% in different district will decrease the printing result.

- This SAV product is with permanent glue and have the possibility of residual gum with different substrate and pasting period. Advise to use the same batch product to joint.

Product Application：