NZ3509G

Transfer Film

Description：

Film:      65 micron transparent PVC film

Adhesive： transparent adhesive

Liner：    100gsm white PEK paper with one side PE & silicon coating

Width：   0.914/1.06/1.22/1.27/1.37/1.52m

Features：

1.  Low-viscosity movable adhesive, no glue residue, which can transfer 100% of the picture to the carrier to be displayed.

2.  Fast transfer, high transparency, simple operation and easy construction.

Applications：

- Effectively transfer patterns to printed articles.

- Suitable for various advertising and decoration fields, such as carved paintings and car sticker.

Technical Data：

Testing condition: Indoor temperature 23±2°C; Relative humidity 50±5%.

| Test Items | Units | Test method | Average value |
| --- | --- | --- | --- |
| Thickness PVC Weight-Liner Weight -finished product Initial Adhesion Tensile strength MD Tensile strength CD Construction Temperature Applicable Temperature | Micron g/m² g/m² N/25mm N/25 mm N/25 mm °C °C | GB/T6672-2001 GB4669-1995 GB4669-1995 FTM 9 GB/T1040.1-2006 GB/T1040.1-2006 | 65±10 100±10 200±20 ≥0.5 ≥20 ≥15 20±10 -20 ~ +70 |

- All technical data is subject to change without prior notice.

Storage Condition：

All NAR products always need to be stored in the original packing and with the original protection materials, preferably stored hermetically, no more than 6 layers if stored horizontally. Do not expose in direct sunlight or heat sources. The shelf life of the product is one year under this condition.

Production Environment：

- Temperature of 25 ± 5 °C, relative humidity of 50%±10%, clean dust-free environment without suspended matter.

- Follow-up operation shall be carried out after the pattern is completely transferred.

Warranty Condition：

1.  One year shelf life: stored in suitable conditions, preferably use within 6 months;

2.  One year prosecution period: from the product manufacture date, no-acceptance for overdue product.

Important Remark：

The information mentioned in this product data sheet is based upon tests that were executed by NAR, and that we consider to be reliable. The information always represents an average, a minimum or a maximum value. It is only for your reference, and does not give any guarantee. It is up to the end user to decide whether or not the product is suitable for the particular application.

Product Application：